Safety Note: Thermal Runaway & Chemistry Selection for Eldercare Platforms

Thermal Runaway Behavior: 18650 (NMC/NCA) vs. LiFePO4 (LFP)

- Standard 18650 (Lithium-Ion): While offering superior energy density, typical NMC/NCA cells have a relatively low thermal runaway onset temperature (approx 150 C). Critically, when the cathode breaks down during a thermal event, it releases internal oxygen. These self-fuels the combustion process, making the resulting fire extremely volatile and difficult to extinguish.

- LiFePO4 (Lithium Iron Phosphate): LFP chemistry boasts a significantly higher thermal runaway threshold (approx 270 C). More importantly, the strong P-O covalent bonds within the cathode prevent the release of oxygen even under severe abuse conditions (e.g., short-circuit or physical puncture). While an LFP cell may vent smoke if catastrophically damaged, it typically will not ignite or explode.

Recommendation for Fari-Class Platform:

For an indoor eldercare assistant like Fari, LiFePO4 is the mandatory choice. The primary demographic (the elderly) has limited mobility and increased evacuation times. The catastrophic risk of an oxygen-fueled lithium fire indoors completely outweighs the volume and weight penalties associated with LFP's lower energy density. Absolute thermal stability must supersede runtime optimization in this specific product segment.